## Slide 1: HGCAL Hamburg Model Analysis

## Slide 2: HGCAl 2.2 Front (43 min)
Fitted parameters include (beneficial annealing introduction rate), (reverse annealing introduction rate), (beneficial annealing time constant), (reverse annealing time constant), (stable damage)
At ~ 17 minutes DIODE registers 9.54E+14 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 504 minutes

## Slide 3: HGCAl 2.2 back (43 min)
At ~ 90 minutes DIODE registers 1.35E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 6.01 minutes

## Slide 4: HGCAl 2.3 Front (86 min)
At 0 minutes DIODE registers 2.08E+15 fluence (1 MeV n/cm^-2)
Not able to make a fit to the Hamburg Model, because the front HGCAL cutout experience so much annealing during irradiation
Equivalent annealing at 60C:
  Front: 374 min
  Back: 5.62 min

## Slide 5: HGCAl 2.3 back (86 min)
At ~ 40 minutes DIODE registers 2.78E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C:
  Front: 374 min
  Back: 5.62 min

## Slide 6: HGCAl 2.4 Back (216 min)
At 0 minutes DIODE registers 1.84E+16 fluence (1 MeV n/cm^-2)
Front HGCAL & D0 Diodes Destroyed during Irradiation
Depletion Hit 1000 V’s for first two annealing steps, thus the overlapping data
Not able to make a fit to the Hamburg Model, because the back HGCAL cutout experience so much annealing during irradiation
Equivalent annealing at 60C:
  Front: 106,709 min
  Back: 27,252 min

## Slide 7: HGCAl 2.5 Front (86 min)
At ~60 minutes DIODE registers 2.81E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 69.17 minutes

## Slide 8: HGCAl 2.5 back (86 min)
At ~80 minutes DIODE registers 3.09E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 11 minutes

## Slide 9: HGCAl 2.6 Front (118 min)
At 0 minutes DIODE registers 2.86E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 739.3 minutes

## Slide 10: HGCAl 2.6 back (118 min)
At 80 minutes DIODE registers 5.30E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 20.6 minutes

## Slide 11: HGCAl 2.7 Front (43 min)
At 80 minutes DIODE registers 1.51E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 12.6 minutes

## Slide 12: HGCAl 2.7 back (43 min)
At ~80 minutes DIODE registers 1.27E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 13.09 minutes

## Slide 13: HGCAl 2.8 Front (32 min)
At 80 minutes DIODE registers 1.06E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 14.4 minutes

## Slide 14: HGCAl 2.8 back (32 min)
At 80 minutes DIODE registers 1.05E+15 fluence (1 MeV n/cm^-2)
Equivalent annealing at 60C is 10.9 minutes

## Slide 15: Total Results
Yellow indicates fluence flipping
Need to anneal and measure D0 2.7 & 2.8 (today)
Need to analyze temp profiles for 2.7 & 2.8
Will add Foils to this sheet, will include in HEP shared drive today